SHORT FORM SPECIFICATION 

SECTION 07214

FOAMED-IN-PLACE MASONRY WALL INSULATION
PART 1  -  GENERAL


DESCRIPTION OF WORK:



A.
Applications of insulation specified in this section include the following:




Foamed-In-Place masonry insulation for thermal, sound and fire resistance values.



QUALITY ASSURANCE:




A.
Insulation shall be installed as per manufacture’s recommendation and must come from 


the manufacturer pre-mixed to ensure consistency.  Upon request,  a one year product 


and installation warranty will be issued by  both the manufacturer and installer.



B.
Engage an experienced dealer/applicator who has been trained and licensed by the 


product manufacturer and which has not less than three years direct experience in the 


installation of the product used.

PART 2  -  PRODUCTS


ACCEPTABLE MANUFACTURERS



A.
"Core-Fill 500TM" as manufactured by Tailored Chemical Products, P.O. Box 4186,
 

Hickory, N.C. 28603,  (800) 627-1687.  No substitutions allowed.



MINIMUM PRODUCT PERFORMANCE STANDARDS

(1) Surface Burning Characteristics:  Maximum flame spread, smoke developed and fuel contributed of 0, 5 and 0 respectively.  (2)  Combustion Characteristics:  Must be noncombustible, Class A building material.  (3) Thermal Values:  "R" Value of greater than 3.5/inch @ 75 degrees F mean; ASTM C518-21.  (4)  Sound Abatement:  Minimum Sound Transmission Class ("STC") rating of 53 and a minimum Outdoor Indoor Transmission Class ("OITC") rating of  44 for 8" wall assembly ASTM E90-90).

PART 3  -  EXECUTION


INSTALLATION GUIDELINES



Fill all open cells and voids in hollow concrete masonry walls where shown on drawings.  The 

foam insulation shall be pressure injected through a series of  5/8" to 7/8" holes drilled into 

every vertical column of block cells (every 8" on center) beginning at an approximate height of  

four (4) feet from finished floor level.  Repeat this procedure at an approximate height of  ten 

(10) feet above the first horizontal row of  holes (or as needed) until the void is completely filled.  

Patch holes with mortar and score to resemble existing surface.

